Unconfined Compression Test

Abridged version (you are to combine with Bowles, Chapter 14, page 155)

- Weigh out about 1.2 kg of soil and pass through a #10 sieve

- Add about 11 % water and mix thoroughly.  Do your best to eliminate all small soil balls.

- Take about 600 grams of the soil you just mixed and another 7% moisture, mix thoroughly.

- Make two compacted samples for each mix, 11% and 18%, using the Harvard Miniature compaction apparatus.

  - This is similar to the proctor compaction test.

  - Three layers of soil, score between each layer (this is important).

  - 25 blow with the Harvard compacter between each layer.

  - Jack out the soil from the Harvard tube with the soil jack.

- The L/d ratio must be 2 < L/d < 2.5 otherwise your results will not be true to the test. See page 158 of lab book.

  - L/d must be large enough to avoid interference of potential 45o planes.

  - L/d must be small enough to avoid a "column" failure

- Weight sample.

- Set up data sheet.  See that you are set to take reading at 10, 20, 50, 100, 150, 200, 250….etc from the Deformation dial (0.001 in)

- Make certain you understand the load dial and how to calculate loads.

- Determine the crank rate.

  - You want a strain rate of 1/2 to 2% per minute.

  - Therefore for a 2-inch sample you would want a crank rate of about 0.02 in./min.

- READY TO GO (check with Prof. Kney before you begin)

- Three ways you know you have reached failure.

  - Load dial decreases

  - Load dial remains constant

  - Deformation is past 15% strain, say 20 to 25%.  Calculate this point before you start.

- Be certain to draw a picture of the failed sample

- Don't forget to take moisture content samples.